## Slide 1: AFLOW: Integrated infrastructure for computational materials discovery
COREY OSES DAVID HICKS MARCO ESTERS RICO FRIEDRICH
ANDRIY SMOLYANYUK CORMAC TOHER
STEFANO CURTAROLO
Materials Science Duke University

## Slide 2: AFLOW School Team
Corey Oses
Cormac Toher
David Hicks
Marco Esters
Andriy Smolyanyuk
Stefano Curtarolo
Rico Friedrich

## Slide 3: AFLOW School Zoom Logistics
Microphone should be muted if not speaking
If you have a question, use the Chat or Raise Hand functions

## Slide 4: AFLOW School Zoom Logistics
Reactions button
Raise hand button

## Slide 5: AFLOW School Zoom Logistics
Raised hand button

## Slide 6: AFLOW School Zoom Logistics
Exercises will be part of each session
For exercises, group will be separated into breakout rooms within Zoom
One instructor will be in each breakout room, and you can ask this instructor for assistance, share your screen with them, etc.
Exercise materials are available in the TU Dresden VNC portal – to access the portal, you will need to install and run the TU Dresden VPN: https://tu-dresden.de/zih/dienste/service- katalog/arbeitsumgebung/zugang_datennetz/vpn#
Follow instructions for your operating system

## Slide 7: AFLOW School Zoom Logistics
Once VPN is connected, log into VNC virtual machine using link and password sent to you by email
Please do not use the “Log out” function, as this will shut down the VM for everyone
Please do not shut down the VM
To exit, simply close the browser window/tab
Please do not change the resolution in the desktop environment

## Slide 8: AFLOW School Zoom Logistics
Connect to Virtual Machine

## Slide 9: AFLOW School Zoom Logistics
Use password sent to you by email

## Slide 10: AFLOW School Zoom Logistics
Clipboard and screen resizing

## Slide 11: AFLOW School Zoom Logistics
Open clipboard to copy/paste into Portal
Use clipboard to copy/paste into Portal

## Slide 12: AFLOW School Zoom Logistics
Settings
Clip to Window Scaling mode
Remote Resizing

## Slide 13: AFLOW School Zoom Logistics
Terminal
Home directory

## Slide 14: AFLOW School Zoom Logistics
AFLOW Exercises directory

## Slide 15: Novel Materials Applications
Thermal barrier coatings: energy/aerospace
Superhard, wear resistant coatings: machine tools
Biocompatible, corrosion resistant alloys: medical implants
Photovoltaic materials: solar energy harvesting
Superconductors and heat sinks for advanced electronics
Solid state electrolyte: Li-ion batteries

## Slide 16: Challenge: materials space
78
◆
2
= 3, 003
78
◆
3
= 76, 076
78
◆
4
= 1, 426, 425
78
◆
5
= 21, 111, 090
78
◆
6
= 256, 851, 595

## Slide 17: Challenge: materials space
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017), D. Hicks et al., Comput. Mater. Sci. 161, S1-S1011 (2019)

## Slide 18: Challenge: materials space
10177
M. J. Mehl et al., Comput. Mater. Sci. 136, S1-S828 (2017), D. Hicks et al., Comput. Mater. Sci. 161, S1-S1011 (2019)

## Slide 19: Automated Materials Discovery
Automated computational materials discovery:
Experimental structures Automated QM calculations
19
Searchable/sortable database
Candidate materials
Structural prototypes
ML models
Density functional theory
http://www.aflow.org

## Slide 20: AFLOW: Automatic FLOW
AFLOW
DFT-code
aflow.in
Elastic
Electronic
Thermal
Storage
Property calculation
Database storage
Calculation management
Input file generation
DFT-
code
DFT-
code
DFT-
code
ERROR?
AFLOW source code now available under GPL 3 materials.duke.edu/AFLOW/
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Calderon et al., Comput. Mater. Sci. 108A, 233 (2015)

## Slide 21: AFLOW.org: web portal
> 3.5 million entries
> 700 million properties
breakdown of properties
aflow.org
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Calderon et al., Comput. Mater. Sci. 108A, 233 (2015)
AFLOW
Schools and Seminars

## Slide 22: AFLOW.org: seminars
22
Seminar sign-up link
Online seminars hosted by Center for Autonomous Materials Design
Seminars take place every two weeks on Thursday afternoons
See aflow.org/seminars/ for more details

## Slide 23: AFLOW.org: applications
23
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Calderon et al., Comput. Mater. Sci. 108A, 233 (2015)
aflow.org

## Slide 24: AFLOW.org: search page
Element selection
Number of species
Element group selection
Logic operations
aflow.org/search/
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 25: AFLOW.org: search page
Slide to Property Filters
Bring property filters onto search page
aflow.org/search/
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 26: AFLOW.org: search page
Property Filters
aflow.org/search/
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 27: AFLOW.org: search page
Selected Elements
Number of species=2
Added filter for Egap: electronic band bap
Check box to restrict search results to specific value range
Select “Add” to add filter
aflow.org/search/
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014)

## Slide 28: AFLOW.org: search page
28
Exercises:
Use the advanced search functionality to find the band gap for SiC in the zincblende structure (space group number 216).
Use the advanced search functionality to find the materials containing Sn but not Pb with band gaps between 1 eV and 3 eV in the ICSD catalog of the AFLOW database. How many results are returned?
Alternative server: aflowlib.duke.edu/search/ui/
R. H. Taylor et al., Comput. Mater. Sci. 93, 178-192 (2014), F. Rose et al., Comput. Mater. Sci. 137, 362 (2017)

## Slide 29: Objective 1: Stability screening
29
elements + arrangements
Thermodynamic stability
0.8
0.6
0.4 0.2
50
0
≠50
≠100
≠150
≠200
Zr
1≠250
0.8
0.6
0.4
0.2
1001
≠2500
50
0
≠50
≠100
≠150
≠200
Cu
formation enthalpy (meV/atom)
Cu5Zr
Cu10Zr7
Cu2Zr
CuZr2
aflow.org
0100
C. Oses et al., J. Chem. Inf. Model. 58(12), 2477-2490 (2018)

## Slide 30: Objective 1: Stability screening
elements + arrangements
Mechanical stability

## Slide 31: Objective 2: Design rule discovery
Mo6PbS8
Mo6NdS8
A
B
X3
ABX3 [X = F, O]
ABF3
ABO3
 / B
 / A
Example 2: thermal conductivity in perovskites
Example 1: superconducting critical temperature
A. van Roekeghem, J. Carrete, C. Oses,
S. Curtarolo, and N. Mingo, Phys. Rev. X 6, 041061 (2016).
O. Isayev, D. Fourches, E. N. Muratov, C. Oses,
K. Rasch, A. Tropsha, and S. Curtarolo, Chem. Mater. 27(3), 735-743 (2014).
TC "
TC #

## Slide 32: Objective 3: Machine learning models
crystal structure
Electronic Proper1es
Thermo-Mechanical Proper1es
metal or
i
nsulator?
no EBG
{EBG E R :
EBG > 0}
band gap energy predic4on
bulk modulus (VRH)
predic4on
{X E R}
yes
no
classiﬁca4on model
regression model
regression models

## Slide 33: AFLOW: Installation
33
AFLOW can be used on Linux, Mac, and Windows
Windows requires additional software:
  Windows Subsystem for Linux (Windows 10)
  Cygwin (other Windows versions)
For instructions and installation scripts, visit:
http://aflow.org/install-aflow/
Curtarolo et al., Comput. Mater. Sci. 58, 218 (2012); Curtarolo et al., Comput. Mater. Sci. 58, 227 (2012)

## Slide 34: Outline: Day 1
Keynote address: To mix or not to mix? Synthesizability entropy-descriptors and the controversial role of vibrations in the stability of high-entropy ceramics (S. Curtarolo)
Session 1: DFT+AFLOW (C. Oses & D. Hicks)
  VASP input files
  Energy calculations and k-point convergence
  Primitive and conventional cell representations
  Spin-polarized calculations
  Density of states and band structure calculations
  AFLOW input file: aflow.in
  Configuration file: aflow.rc
  Managing ab-initio calculations

## Slide 35: Outline: Day 2
Session 2: Symmetry (D. Hicks)
  AFLOW-SYM algorithm
  AFLOW-SYM output files
  AFLOW-SYM command line interface
  AFLOW-SYM Python wrapper
  Brillouin zone and AFLOW Standard k-path
  AFLOW-SYM via AFLOW-Online
Session 3: Structure prototyping (D. Hicks)
  Resolving material/structural prototypes
  AFLOW Crystal Prototypes (encyclopedia)
  AFLOW prototype generation

## Slide 36: Outline: Day 3
Session 4: Thermodynamic stability (C. Oses)
  Identifying stable vs. unstable structures
  Applications: Rare-earth free Heusler magnets
  AFLOW-CHULL
Session 5: Thermodynamics of polar materials (R. Friedrich)
  Thermodynamic stability of polar materials: CCE
  Application: Thermodynamic stability of ternary oxides and halides
  AFLOW-CCE
Session 6: Disorder (C. Oses)
  Resolving material/structural prototypes
  AFLOW-POCC: Ensemble average properties
  AFLOW-POCC algorithm
  AFLOW-POCC via AFLOW-Online
  AFLOW-POCC command line interface

## Slide 37: Outline: Day 4
Session 7: Thermomechanical properties (C. Toher)
  AFLOW-AEL: Elastic properties
  AFLOW-AGL: Debye model
Session 8: AFLOW.org database and APIs (M. Esters)
  AFLOW.org database structure
  AFLOW REST-API
  AFLUX: AFLOW Search API
Session 9: Machine Learning (C. Toher)
  PLMF representation
  AFLOW-ML API

## Slide 38: Outline: Day 5
Session 10: AFLOW-XtalFinder (D. Hicks)
  AFLOW-Xtalfinder algorithm
  AFLOW-Xtalfinder command line interface
  AFLOW-Xtalfinder Python wrapper
Session 11: Phonons in the Harmonic Approximation (M. Esters)
  Introduction to phonons
  AFLOW-APL: Phonon dispersions and phonon DOS
  AFLOW-APL: Thermodynamic properties from phonons
  AFLOW-APL: Visualizing atomic displacements
Session 12: The Quasi-Harmonic Approximation (A. Smolyanyuk)
  Introduction to the quasi-harmonic approximation
  AFLOW-QHA: Calculating and visualizing thermodynamic properties