## Slide 1: Structural analysis and generation of materials: AFLOW-SYM, AFLOW Prototype Encyclopedia, and AFLOW-XtalFinder
v
David Hicks
AFLOW – Johns Hopkins University
Session 2
Wednesday, September 21st, 2022
Advanced Research Computing at Hopkins

## Slide 2: Structure features for ML
structural tools to aid ML training and generate hypothetical materials
PtSbSc
PtSbTb
PtSbHo
S2
C4
features for training
structure analysis
ML
feature vectors
train new models
crystal generation engine
prototype
Egap

## Slide 3: AFLOW-SYM
a
b
mirror
n-fold
xi
xj
✓
AFLOW-SYM tests invariance of crystal under transformations
Hicks et al., Acta Cryst. A74, 184 (2018)
Pearson symbol
space group
Bravais lattice
Wyckoff positions
conventional cell
descriptions:
primitive cell
…

## Slide 4: Identifying symmetry elements
mapped?
mapped
mapped
✕ not mapped
4-fold rotation (90o)
attempt symmetry operation
Hicks et al., Acta Cryst. A74, 184 (2018)
radius (threshold for mappings)
||xorig - xtransformed||  ✏
periodic boundary conditions
mappings in non-uniform metric spaces

## Slide 5: Algorithm improvements
fractional
demin
f
cartesian
✓
nˆm
dmin
c
demin
c
robust mapping procedure
accurate in both direct and reciprocal spaces
cartesian fractional
adaptive tolerance scheme
ensures self-consistent symmetry
0
1.0
0.5
0.3
b
0.1
✏0
✏new
rhl SG #166
fcc SG #225
mcl SG: #11
orc SG #59
single global tolerance
system-specific tolerance
atomic position resolution
nearest-neighbor analysis
Hicks et al., Acta Cryst. A74, 184 (2018)

## Slide 6: Benchmark with existing packages
Mismatch with respect to space group listed in description of experimental structure in ICSD
Hicks et al., Acta Cryst. A74, 184 (2018)

## Slide 7: Crystallographic symmetry
Calculates the relevant symmetry groups for crystallographic structures
lattice point group
reciprocal lattice point group (BZ symmetry) factor group (unit cell symmetry) crystallographic point group
dual of crystallographic point group (IBZ symmetry)
Patterson symmetry group space group
site point group (atom point symmetry)
Hicks et al., Acta Cryst. A74, 184 (2018)

## Slide 8: Symmetry descriptions
Hicks et al., Acta Cryst. A74, 184 (2018); Hahn, Kluwer Academic Publishers (2002)
consistent with International Tables for Crystallography (ITC)
standard space group label
space group setting
Wyckoff positions
Ag 4 a 0, 0, 0
space group number (1-230)
225
International (Hermann-Mauguin)
𝐹𝑚3#𝑚
Schoenflies
𝑂"
!
Hall symbol
𝐹 4/𝑚 −3 2/𝑚
Pearson symbol
cF4
Ag 0, 0, 0
Ag 0, 1/2, 1/2
multiplicity
letter designation
representative coordinate
expand coordinates
Ag 1/2, 0, 1/2 Ag 1/2, 1/2, 0
8

## Slide 9: AFLOW-SYM: online
visualize symmetry operations on entry pages of aflow.org
online functionality aflow.org/aflow-online

## Slide 10: Navigate to AFLOW-Online (aflow.org/aflow-online)

## Slide 11: AFLOW Crystal Prototype Encyclopedia

## Slide 12: AFLOW: Crystallographic prototypes
AFLOW contains built-in structural prototypes:
Decorating prototypes with different elements allows for automated creation of new hypothetical materials
~1,100 prototypes available at aflow.org/prototype-encyclopedia
Prototype T0001: Heusler structure
Prototype T0002: Anti-Heusler structure
Prototype T0003: Half-Heusler structure
Mehl et al., Comput. Mater. Sci. 136, S1 (2017); Hicks et al., Comput. Mater. Sci. 161, S1 (2019); Hicks et al., Comput. Mater. Sci. 199, 110450 (2021)

## Slide 13: Crystal Prototype Encyclopedia
part 1
288 prototypes
part 2
302 prototypes
1,100
prototypes
Strukturbericht
space group
Wyckoff positions
The AFLOW Prototype Encyclopedia
prototypes are integrated into AFLOW software = automatic materials generation
standard label
historic labels
explicit coordinates
Pearson symbol
lattice vectors
similar compounds
content
visualizations
part 3
510 prototypes
Mehl et al., Comput. Mater. Sci. 136, S1 (2017); Hicks et al., Comput. Mater. Sci. 161, S1 (2019); Hicks et al., Comput. Mater. Sci. 199, 110450 (2021)

## Slide 14: Standard designation and generation
3.823,1.638,0.375,0
3.823,1.638,0.270,0
3.823,1.099,0.375,0
AFLOW label
Descriptive label and method for generation (e.g., wurtzite)
AFLOW parameters
degrees of freedom consistent with symmetry
AB_hP4_186_b_b
a
c/a
z1 z2
reduced stoichiometry
species A
Wyckoff letter(s)
species B
Wyckoff letter(s)
Pearson symbol
space group number
Mehl et al., Comput. Mater. Sci. 136, S1 (2017); Hicks et al., Comput. Mater. Sci. 161, S1 (2019); Hicks et al., Comput. Mater. Sci. 199, 110450 (2021)

## Slide 15: Navigate to Prototype Encyclopedia (aflow.org/prototype-encyclopedia)

## Slide 16: Online application
www.aflow.org/prototype-encyclopedia
search by structure descriptors
Jmol viewer
general prototype info
Mehl et al., Comput. Mater. Sci. 136, S1 (2017); Hicks et al., Comput. Mater. Sci. 161, S1 (2019); Hicks et al., Comput. Mater. Sci. 199, 110450 (2021)

## Slide 17: Online application
prototype generator
17
lattice and atom information (symbolic notation)
www.aflow.org/prototype-encyclopedia
Mehl et al., Comput. Mater. Sci. 136, S1 (2017); Hicks et al., Comput. Mater. Sci. 161, S1 (2019); Hicks et al., Comput. Mater. Sci. 199, 110450 (2021)

## Slide 18: AFLOW-XtalFinder

## Slide 19: Search for structural diversity
lattice and origin choices obfuscate similarity
programmatically search for distinct structures in datasets
mitigate duplicates
data mining (statistics)
machine learning
identify prototypes
decorate structures
materials discovery
AFLOW-XtalFinder
Ex:
Hicks et al., npj Comput. Mater. 7, 30 (2021)
19

## Slide 20: Autonomous prototype finder
IDENTIFICATION: find prototype of crystalline material
Hicks et al., npj Comput. Mater. 7, 30 (2021)
0
0.5
self-consistent crystal prototype finder
0.25
scan
✏sym

## Slide 21: Structural uniqueness
S2
C4
S2
isopointal structures
Hicks et al., npj Comput. Mater. 7, 30 (2021)
a
local geometry comparison
coordination analysis
symmetry comparison
geometric comparison
local LFA geometry
matched or unmatched atoms
lattice differences
dmap
similarity metrics
local snapshots
isoconfigurational
2
@
00
S = 1
1 0
0 0
0 0 1
A
4
@
00
C = 1
-1 0
0 0
0 0 1
A
. . .
@
00
1 0
S = 1 0 0
0 0 1
A
4
@
00
C = 1
-1 0
0 0
0 0 1
C4
A
. . . 2
lattice + origin search
21

## Slide 22: Compare against repositories
compare to Prototype Encyclopedia
Mehl et al., Comput. Mater. Sci. 136, S1 (2017); Hicks et al., Comput. Mater. Sci. 161, S1 (2019); Rose et al., Comput. Mater. Sci. 137, 362 (2017); Hicks et al., npj Comput. Mater. 7, 30 (2021)
22
?
label: ABC_cF12_216_b_c_a common name: half-Heusler Strukturbericht: C1b
web: aflow.org/prototype-encyclopedia/ ABC_cF12_216_b_c_a.html
matching entry
input structure
compare to AFLOW database
database (via AFLUX)
?
ccoommppoouunndd | aauuiidd | mmiissfifitt | Hatom (eV/atom)
CCll11NNaa11 | aaflflooww::eecc2233002299aa1188dd33ffeecc99 | 00..0000338844 | -3.39049
CCll11NNaa11 | aaflflooww::bb22eecc44bb6688ee1122ff33667744 | 00..0000441155 | -3.39056
CCll11NNaa11 | aaflflooww::11335544bbbbeeff44eedddd8800bb33 | 00..0000339944 | -3.39032
CCll11NNaa11 | aaflflooww::11ccdd7711111144997722dd4466dddd | 00..0000552255 | -3.39078
CCll11NNaa11 | aaflflooww::99001177ff99cc6644eeaadd2222aabb | 00..0000444455 | -3.39062
input structure
compare user structure sets
automatically groups similar structures
structure similarity vs properties

## Slide 23: Navigate to AFLOW-Online (aflow.org/aflow-online)

## Slide 24: Exercises
Navigate to http://aflow.org/prototype-encyclopedia/A2B7C2_tI44_119_i_bdefgh_i. Generate a geometry file with the default parameters and calculate the space group on http://aflow.org/aflow-online? What space group(s) do you find if you change the tolerance from “tight” to “loose”?
Navigate to the following AFLOW entry: http://aflow.org/material/?id=aflow:44368cc42c6f60cc. At the bottom of the page, click on the “VASP-CONTCAR” under “Relaxed Structure” and copy the geometry file. On AFLOW-Online, determine the prototype designation via the “AFLOW prototype” button. How many degrees of freedom are there (i.e., # of parameters)?
Navigate to the rock salt prototype page (https://aflow.org/prototype-encyclopedia/AB_cF8_225_a_b.html). Generate a sodium chloride crystal with the default parameters. On AFLOW-Online (http://aflow.org/aflow- online), use the “Compare to library” button and “Compare to AFLOW database” method and “Submit”. How many AFLOW entries match to the input? (HINT: Check for “compounds_duplicate=” in the output.)

## Slide 25: Python modules
First, download AFLOW source code: http://aflow.org/install-aflow/
Generate Python modules via AFLOW command:
aflow --aflow_sym_python
AFLOW-SYM:
AFLOW-XtalFinder:
aflow --aflow_xtalfinder_python
Example scripts and functionality at http://aflow.org/aflow-schools

## Slide 26: More information
For more functionality, download AFLOW source code: http://aflow.org/install-aflow/ READMEs:
aflow --readme=symmetry
Relevant articles:
aflow --readme=prototypes
aflow --readme=xtalfinder
D. Hicks, C. Oses, R.H. Taylor, E. Gossett, G. Gomez, C. Toher, M.J. Mehl, O. Levy, and S. Curtarolo, AFLOW-SYM: Platform for the complete, automatic and self-consistent symmetry analysis of crystals, Acta Cryst. A74, 184-203 (2018). doi: 10.1107/S2053273318003066
AFLOW-SYM:
Prototypes:
M.J. Mehl, D. Hicks, C. Toher, O. Levy, R.M. Hanson, G.L.W. Hart, and S. Curtarolo,
The AFLOW Library of Crystallographic Prototypes: Part 1, Comp. Mat. Sci. 136 Supplement, S1–S828 (2017). doi: 10.1016/j.commatsci.2017.01.017
D. Hicks, M.J. Mehl, E. Gossett, C. Toher, O. Levy, R.M. Hanson, G.L.W. Hart, and S. Curtarolo,
The AFLOW Library of Crystallographic Prototypes: Part 2, Comp. Mat. Sci. 161 Supplement, S1-S1011 (2019). doi: 10.1016/j.commatsci.2018.10.043
D. Hicks, M.J. Mehl, M. Esters, C. Oses, O. Levy, G.L.W. Hart, C. Toher, and S. Curtarolo,
The AFLOW Library of Crystallographic Prototypes: Part 3, in press, Comp. Mat. Sci. (2021). arXiv:2012.05961
AFLOW-XtalFinder:
D. Hicks, C. Toher, D.C. Ford, F. Rose, C. De Santo, O. Levy, M.J. Mehl, and S. Curtarolo, AFLOW-XtalFinder: a reliable choice to identify crystalline prototypes, npj Comput. Mater. 7, 30 (2017). doi: 10.1038/s41524-020-00483-4